## Slide 1
Introduction to Waveguide Optics
Jiří Čtyroký ctyroky@ufe.cz
Institute of Photonics and Electronics AS CR, v.v.i., Prague, Czech Republic

## Slide 2
Where I come from…
Institute of Photonics and Electronics AS CR, v.v.i.
Academy of Sciences of the Czech Republic is a non-university institution for basic and applied research consisting of 54 independent institutes

## Slide 3
optical fibre
channel optical waveguide
optická vlákna
Examples of waveguide structures
photonic crystal waveguide
etc…
loss
gain
“ARROW” (antiresonant reflecting OW)
“gain/loss” waveguide
subwavelength grating waveguide
longitudinally uniform
longitudinally periodic
metal
plasmonic waveguide
microring
resonator
angularly
uniform

## Slide 4
Theoretical fundamentals of optical waveguides
Planar waveguides; waveguide modes, their properties. Guided and leaky modes. Other types of waveguiding, guiding by a single interface
Waveguide bends, whispering-gallery modes, circular resonators
Channel waveguides, approximate analytical methods.
More complex waveguide structures. Fundamentals of a rigorous coupled-mode theory
Introduction to modal methods; transfer matrix method, basics of the film mode matching
Periodic media, Bloch modes, origin of the bandgap, SWG waveguides, (photonic crystals)
“Canonical” waveguide structures: Y-junctions, directional coupler, two- and multimode interference couplers, microresonators
Plasmonic waveguides and structures. Surface plasmon sensing. Hybrid dielectric-plasmonic slot waveguide, plasmonic devices
Waveguide structures with loss and gain; asymmetric grating couplers, (“PT-symmetric” waveguide structures)
…
Basic requirements: Theory of electromagnetic field, Maxwell equations
Tentative list of topics

## Slide 5
Basic math & phys background
Dielectric (possibly also metallic) non-magnetic linear source-free medium,
time-harmonic dependence of electromagnetic field:
Plane-wave solution:
complex wave vector

## Slide 6
Field at the interface between two media
TE polarization
TM polarization
Plane wave incident on a planar interface
Field continuity conditions at

## Slide 7
Fresnel coefficients
total reflection
Brewster angle
critical angle
|RTE|, |RTM|
Angle of incidence (deg)
“region of interest” of waveguide optics
Angle of incidence (deg)
arg(RTE), arg(RTM)

## Slide 8
The simplest waveguide: two (perfect) conductors
perfect conductors
Two equivalent physical pictures: 1. a series of successive reflections of a plane wave
2. two plane waves propagating upwards and downwards
In both cases, the “nonzero wave” in the waveguide can exist only under the “condition of transverse resonance”
Waves can thus propagate only as discrete waveguide modes with propagation constants
The transverse field distributions have the forms
(for TM only)
… polarization degeneracy
(except for m = 0)

## Slide 9
Dielectric slab waveguide
Condition of transverse resonance:
Total reflection at both interfaces:
or
Dispersion equation for Nm shows polarization birefringence,

## Slide 10
Effective thickness & “period of propagation”
Total internal reflection is linked up with the Goos-Hänchen shift,
(and a similar, somewhat more complicated expression for TM) – effective thickness
… “period of propagation”
These “ray-optic concepts” are useful also for inherently “wave-optic” phenomenon of optical waveguiding.

## Slide 11
Dispersion diagram (examples)
Asymmetric waveguide
Symmetric waveguide
Number of TE and TM modes identical,
TE0 and TM0 always exist
All modes exhibit cut-off

## Slide 12
Distribution of modes of a slab waveguide

## Slide 13
Electromagnetic theory of a slab waveguide
1. TE polarization:
2. TM polarization:
Planar waveguide as a structure with 1D permittivty distribution:
Eigenmode field:
Eigenvalue equations for eigenfunctions and eigenvalues

## Slide 14
Analogy between a planar waveguide and a potential well in quantum mechanics
guided modes
substrate mode
radiation mode
bound states
reflection from the potential barrier
free particle
Field equation for a TE mode in a planar waveguide
Schrödinger equation for a particle in a potential well
There is not such an exact analogy for TM polarization, but its behaviour is very similar

## Slide 15
Guiding of optical radiation in a dielectric waveguide
Guided modes:
Radiation (substrate) modes:
Radiation modes (superstrate):
guided mode
substrate
mode
superstrate
mode
guided mode
“substrate” mode
radiation mode

## Slide 16
Orthogonality of eigenmodes
It can be shown that fields of guided modes (from the discrete spectrum) are orthogonal,
For lossless waveguides,
of guided modes are real, and thus
(Only) in this case, eigenmodes are also power-orthogonal:
power carried by a superposition of (guided and non-evanescent radiation) modes is given by the sum of powers of individual modes
For radiation and evanescent modes, the orthogonality condition sounds
Radiation and evanescent modes are always orthogonal to discrete guided modes:
(in the sense of the principal value
of the integral)

## Slide 17
Leaky modes
Leaky modes are not “true” eigenmodes of the waveguide structure but often allow for a simple description and physically understandable interpretation of wave propagation
in waveguide structures with (weak) radiation loss
SOI planar waveguide radiating into the Si wafer
tunelling
“Standard” dispersion relation
(transverse resonance condition)
…“frustrated” reflection coefficient ,
SOI waveguide supports only leaky modes with complex effective indices,
Waveguide with coupling grating as a leaky-mode structure

## Slide 18
Another type of waveguiding – ARROW
M. A. Duguay et al., Appl. Phys. Lett. vol. 49, 13, 1986.
Antiresonant reflecting optical waveguide – ARROW)
Differences between an ARROW and a conventional index-guiding waveguide
refractive index of the guiding layer can be lower than those of the grating
the gratings must operate in the Bragg regime (the 1D photonic crystal has to exhibit a bandgap)
theoretically, ARROW with lower index guiding layer supports only leaky modes; the number of periods has to be sufficient to suppress power leakage through the grating
waveguiding layer (“defect in the photonic crystal”)
Bragg grating (“1D photonic crystal”)
Bragg grating (“1D photonic crystal”)

## Slide 19
Another type of waveguiding – ARROW
M. A. Duguay et al., Appl. Phys. Lett. vol. 49, 13, 1986.
Antiresonant reflecting optical waveguide – ARROW)
Differences between an ARROW and a conventional index-guiding waveguide
refractive index of the guiding layer can be lower than those of the grating
the gratings must operate in the Bragg regime (the 1D photonic crystal has to exhibit a bandgap)
theoretically, ARROW with lower index guiding layer supports only leaky modes; the number of periods has to be sufficient to suppress power leakage through the grating
waveguiding layer (“defect in the photonic crystal”)
Bragg grating (“1D photonic crystal”)
Bragg grating (“1D photonic crystal”)

## Slide 20
Guiding by a single interface
Are two interfaces essential for waveguiding? (Typically yes, but…)
1. Surface plasmon-polariton at dielectric-metal interface
Supported if
power
flow
2. Interface between media with a balance of loss and gain
power
flow
Pole of the reflection coefficient: possible only for TM polarization
Wave is confined if
3. Zenneck wave at the interface of a lossy and lossless media (1907)

## Slide 21
Circularly bent waveguide
M. Heiblum and J. H. Harris, IEEE JQE, vol. QE-11, pp. 75-83, 1975.
Bent waveguide:
Straight waveguide:
Conformal mapping:
Transformed equation:
Very large radius
optical
tunelling
„whispering
gallery“ mode
internal interface
“not necessary”
bent guide
strong bend

## Slide 22
Ring resonator, or bent waveguide?
Polarization:
Helmholz equation:
Bessel equation
angular propagation constant
Field continuity conditions: continuous at :
Separation of variables:
(We are not going to solve this equation!)

## Slide 23
Ring resonator, or bent waveguide?
Dispersion equation:
Frequency introduced “on purpose”
We have two basic possibilities how to proceed:
fix and seek for (complex) azimuthal propagation constant for a bent waveguide, or
fix (as an integer) and seek for (complex) resonant frequency of a ring resonator.
bent waveguide
ring resonator

## Slide 24
Examples of field distributions
disk
ring
(Lossy) resonators
Eigenmodes of dielectric resonators are leaky modes!

## Slide 25
Channel waveguides
Let’s separate transversal and longitudinal field components of an eigenmode:
We obtain a 2D eigenvalue equation
Modes of channel waveguides are hybrid – all field components are generally nonzero
General considerations: vector equation
Weakly guiding waveguide: term is negligibly small; then
…essentially scalar equation, small.

## Slide 26
Marcatili method – separation of variables
Then , and
A very simple approximate mode solving method for 2D waveguides
E.A.J. Marcatili, Bell System Tech Journal 48, 2071-2102, 1969
Approximation of weak guiding,
Simple solution if the profile were separable:
Subtracting from the permittivity in the corners makes the profile separable,
The task is reduced to solving 2 simple 1D equations, but results close to cut-off are questionable.

## Slide 27
Effective-index method for 2D profile
Semi-intuitive method – reduction to a 1D problem
planar waveguide with a vertical profile, effective index N1 and mode field e1(x)
planar waveguide with a vertical profile, effective index N2 and mode field e2(x)
planar waveguide with a vertical profile, effective index N3 and mode field e3(x)
„planar“ waveguide with a lateral profile N1 , N2, N3 and the field e4(y)
The total field is approximately given by the product e(x,y)  e2(x)e4(x).
Advantage: simplicity, clear physical interpretation.
Disadvantage: inaccurate near cut-off, accuracy difficult to assess;
Well-applicable to shallow ridges and diffused channel waveguides,
in many other cases very useful as a first guess. Commonly used method.

## Slide 28
Effective-index method for diffused channel waveguides
Efficient approximate method based on physical intuition.
Suitable for graded-index waveguides and complex structures
Weak guiding, lateral dependence weaker:
Non-separable, but let us try
where “the strong” y-dependence is concentrated in :
is a parameter
Then we solve this equation for several values of and get as an effective lateral profile.
In the next step, we solve the “lateral equation” to get and
What if there is no guided mode for some ? Take the substrate value instead of

## Slide 29
More complex waveguide structures: “rigorous” formulation of the coupled-mode theory
Mode orthogonality:
Wave propagation in the permittivity distribution can be analyzed using the completeness
and orthogonality of the eigenmodes of a waveguide with the permittivity profile
D. Marcuse, Theory of dielectric optical waveguides, 2nd ed. Academic Press, 1991
Eigenmode fields:
Wave in can be expressed as
From Maxwell equations we get the set of first order linear equations for complex amplitudes,

## Slide 30
Slowly varying amplitudes
The coupling constants are given by overlap integrals
Introducing slowly varying amplitudes we obtain

## Slide 31
First-order (Born) approximation
The integrals are “importantly non-zero” only if the integrands do not rapidly oscillate. Thus, if K is slowly vaying, the modes with close propagation constants are strongly coupled . Coupling of modes with significantly different β’s requires that this difference is compensated by rapidly varying K(z).
Supposing slow variation of amplitudes and for small z
Let us formally integrate the set of equations:

## Slide 32
Two simple applications
Let us preserve only “slow” terms satisfying the phase-matching condition:
For slowly-varying amplitudes w can approximately take
Next, we will apply the Taylor expansion for and take only the first two terms:
The spectral dependence of the “transmission coefficient” is approximately given by the Fourier expansion of the spatial dependence of the coupling constant.
We define the “transmission coefficient” from mode to mode and get
1. Coupling of two forward modes

## Slide 33
Waveguide Bragg grating mirror
Boundary conditions:
For
2. Coupling of forward and backward modes by a waveguide grating
Coupled equations:
Solution:
Grating reflectance:

## Slide 34
Spectral dependence of the reflectance

## Slide 35
Numerical methods for modelling waveguide structures
Three main classes of modelling methods:
Frequency-domain mode solvers for calculation of eigenmodes and propagation constants of straight and bent uniform waveguides; 1D, 2D, approximate, “rigorous”; scalar, semivectorial, full-vector; modal methods (Fourier modal method), discretization-based methods like FD, FE. BE, etc.
Frequency-domain “beam propagation” methods (BPM); in principle, scattering methods calculating optical field distribution within a waveguide structure for a given excitation field; modal, FFT-BPM, FD-BPM, FE-BPM; 2D, 3D, scalar, full-vector; unidirectional, bi-directional (in fact, omnidirectional), etc.
Time-domain methods (FDTD , FETD,…): numerical model of optical field generated by a given distribution of sources. Essentially, direct numerical solution of Maxwell equations.
… and many other special methods

## Slide 36
The transfer matrix method
layer l
layer 1
layer L
Matrices are even functions of !
Transformation over the whole multilayer structure:
dispersion
equation
From Maxwell equations applied to a layer l we get
TE
TM

## Slide 37
2D vectorial mode solver
Film mode matching (FMM) (straight guides: Sudbø 1993, 1994, bent guides Prkna 2004)
waveguide cross-section
Transversal refractive index distribution piecewise constant
Subdivide the cross-section into laterally uniform “slices”; each slice represents a multilayer
Find TE and TM modes of each slice
Express total field as superposition of slice modes
Match fields at the boundaries of slices
Stable (impedance or scattering matrix) formalism; fully vectorial solution
Method of Lines (MoL) - requires 1D discretization, FD method school of prof. Reinhold Pregla, Fern-Universität Hagen, Germany

## Slide 38
An example: quasi-TE mode of a rib waveguide

## Slide 39
Film mode matching for circularly bent waveguides
subdivision of the structure into radially uniform “slices”, each “slice” forms a multilayer;
in each “slice”, mode field is expanded into TE and TM modes of a multilayer
field matching at the interfaces between “slices”.
No (or minimum) discretization
Field within the slice described analytically
Treatment analogous to the rectangular case;
radial instead of lateral dependence.
Problem:
Cylindrical functions of complex order instead of trigonometric functions.
L. Prkna, M. Hubalek, J. Čtyroký, IEEE Phot. Technol. Lett. vol. 16, 2057-2059 (2004).
L. Prkna et al., IEEE J. Sel. Topics in Quantum Electr. vol. 11, 217-223 (2005)

## Slide 40
High-contrast SOI microresonator
Quasi-TE00
Quasi-TM00
Quasi-TM10

## Slide 41
Wave propagation in a periodic structure
Photonic analogy of the “Kronig – Penney” model of an electronic crystal
tangential propagation constant (given )
longitudinal prop. constant
TE
TM

## Slide 42
Electromagnetic Floquet – Bloch modes
Transmission through layers 1 and 2 is described by matrices
The matrix for transitin over a single period is evidently
Floquet-Bloch mode is determined as an eigenfunction and eigenvector of
is the prop. const. of the FB mode.
βF is determined up to an additive constant
it is sufficient to determine βF in the interval
 first Brillouin zone.

## Slide 43
Eigenvalues and the photonic bandgap
Let us denote
FB mode is propagating only if
i.e., if
The normalized wavenumber can be explicitly expressed as
If
βF is complex, the wave is attenuated, and the photonic bandgap is created.
eigenvalues of the matrix
are then
outside the bandgap,
within the bandgap

## Slide 44
Band diagrams of a “1D crystal”
“valence”
“conduction”
“dielectric”
“air”
band
band
Brewster angle

## Slide 45
“dielectr.”
band
“air”
band
inside
band
gap
near edge
of the BZ
Electromagnetic Floquet – Bloch modes

## Slide 46
3D analogue – subwavelength grating waveguides
Propagation constant and the effective refractive index of the m-th Bloch mode:
Propagating modes in SWGW are Bloch modes
Grating constant of the SWGW:
“First Brillouin zone” of the SWGW as a 1D photonic crystal:
For lossless propagation,
Group effective index:
In analogy with the behaviour of photonic crystals we expect that
Region of represents the slow light region
(the “bandgap edge”)

## Slide 47
“Canonic” (elementary) waveguide devices

## Slide 48
Elementary waveguide structures
Symmetric Y-junction (1×2 power splitter)
Excitation into the single mode common arm
Power is equally divided between the two output arms due to symmetry

## Slide 49
2. Excitation into a single arm
Symmetric Y-junction excited in the opposite direction
Basic waveguide structures
The antisymmetric mode canot propagate in the single-mode output arm and its power is radiated into the substrate

## Slide 50
2. Excitation into a single arm
Symmetric Y-junction excited in the opposite direction
Basic waveguide structures
Without the second arm, the transmittance is ≤ 100 %

## Slide 51
3. Excitation into both arms with an arbitrary phase shift between the arms
Symmetric Y-junction excited in the opposite direction
Basic waveguide structures

## Slide 52
antisymmetric mode
Asymmetric Y-junction as a mode splitter
symmetric
mode
two-mode waveguide
single-mode arms
Adiabatic splitter: negligibly small mode coupling along the propagation length.
The fundamental mode of the two-mode section remains “fundamental”, etc.
Criterion of asymmetry:
Since cannot be made too large, the decisive role is overtaken by . Typically, for and , the Y-junction behaves “asymmetrically”, for and , the Y-junction behaves as power splitter.

## Slide 53
Symmetric Y-junction
(power divider)
Asymmetric Y-junction (mode splitter)
Spectral bandwidth is limited by the requirements regarding the number of modes; the input and output ports must be single-mode, the central junction double-moded.
The bandwidth 1.2 – 1.6 µm is rather easily attainable.
Application: spectrally independent 2×2 (3-dB) splitter

## Slide 54
Application: spectrally independent 2×2 (3-dB) splitter
Symmetric Y-junction
(power divider)
AsymmetricY-junction (mode splitter)
Spectral bandwidth is limited by the requirements regarding the number of modes; the input and output ports must be single-mode, the central junction double-moded.
The bandwidth 1.2 – 1.6 µm is attainable.
Reversed direction of propagation

## Slide 55
Directional coupler

## Slide 56
Spectral dependence of the directional coupler
Refractive index profile (eff.index)
Distribution of optical intensity
Directional coupler can be used as a (coarse) wavelength demux

## Slide 57
Coupled-mode theory of the directional coupler
Approximate description of the field:
Coupled-mode equations:
Power conservation condition:
- normalized field
Without lost of generality we choose
Boundary conditions:
Solution:

## Slide 58
Two-mode interference coupler
Single-mode I/O ports,
two-mode central section
Similar to directional coupler,
shorter “transfer length” Lt

## Slide 59
Imaging properties of an optical waveguide
Two-conductor waveguide:
Propagation constants in a multimode waveguide:
If
After propagation along a distance L , all modes meet (approximately) with the same phase. The field distribution at z = 0 is then reproduced at z = L. At the halfway, the “image” is reversed.
(inverted image)
O. Bryngdahl and W.-H. Lee, J. Opt. Soc. Am. vol. 68, pp. 310-315, 1978.

## Slide 60
Multimode interference coupler (MMI)
(inverted image)
M.T.Hill, J. Lightwave Technol. 21, 2305-2313, 2003
Advantage:
splitters with small footprint;
Problems:
● dependence in dielectric waveguides is “less parabolic”
phase error for higher-order modes; error is larger for higher refractive-index contrast;
● transversal spatial resolution depends on the number of guided modes with small enough phase errors
Solution:

## Slide 61
Microring resonators
in
through
out
in
through
out
out of resonance
at resonance
microresonator
A. Driessen et al.:"Microresonators as building blocks for VLSI photonics," AIP Proceedings Vol.709, 2003.

## Slide 62
in
through
drop
Basic theory of microring resonators
(Lossless) couplers:
Ring with the perimeter and the (complex) propagation constant :
After elementary manipulations we obtain
At resonance,
Off resonance,
For minimum cross-talk,

## Slide 63
in
through
drop
Spectral properties of a microresonator
Free spectral range
Resonant wavelength
“Finesse”
depends on the group index
Quality factor
intensity
FSR
frequency
drop
thru
Lossless microresonator
intensity
frequency
drop
thru
Lossy microresonator

## Slide 64
Coupling between straight and bent waveguide
Problems:
coupling between guided (lossless) and leaky (radiating) modes
Role of the phase synchronism? (variable relative phase velocities)
Possible approach: linear superposition of mode fields of a straight and bent waveguides:
Finally we obtain a set of first-order coupled-mode equations for complex amplitudes
+ application of some general theorem, e.g., Lorentz-Lorenz reciprocity theorem:
R. Stoffer et al., Opt. Commun., vol. 256, pp. 46-67, Dec 2005.
then successive multiplication by followed by surface integration over S
with coupling “constants” given by overlap integrals of mode fields at .

## Slide 65
Some results of the 3D CMT for the coupling of straight and bent waveguides
R. Stoffer, K. R. Hiremath, M. Hammer, L. Prkna, and J. Čtyroký, "Cylindrical integrated optical microresonators: Modeling by 3-D vectorial coupled mode theory,“ Optics Communications, vol. 256, pp. 46-67, Dec 2005.
Cooperation within 6FP “NAIS”,
University of Twente & IPE AS CR

## Slide 66
Surface plasmons in guided-wave optics

## Slide 67
Surface plasmon(-polariton)
Mutually coupled electromagnetic and charge wave localized at the interface between a dielectric and a metal

## Slide 68
Surface plasmon is a slow wave
SP is a slow wave
Lossless approximation:
factor
It cannot be excited
from the dielectric!!

## Slide 69
Waveguide polarization filter based on resonant excitation of a surface plasmon
J. Čtyroký et al., Proc.10th ECOC’84, pp. 44-45, 1984. (glass, LiNbO3)
J. Čtyroký, H. J. Henning, Electron. Lett. vol.22, 756-757, 1986. (LiNbO3)

## Slide 70
Surface plasmons on a metal layer
J. Čtyroký et al. : Sensors and Actuators B 54, 66–73, 1999.
Mutually coupled surface plasmons
long-range (magn. symmetric)
short-range (magn. antisymm.)
Slightly asymmetric structure
short-range
long-range
short-range
long-range

## Slide 71
Integrated-optic sensor based on surface plasmon resonance

## Slide 72
Field distribution in the waveguide with a section supporting SP

## Slide 73
Experimental arrangement
of a SPR integrated-optic sensor
Refractive index resolution
better than 1.2×10-6
J. Dostalek, J. Čtyroký, J. Homola et al., Sensors and Actuators B-Chemical 76, 8-12 (2001).

## Slide 74
“Bulk” surface plasmon sensor
`
Refractive index resolution of about 1×10-7

## Slide 75
“Plasmonics”
(“photonics” using surface plasmons instead of photonics)
2D guiding of surface plasmons
90° bend
SP enables localization of radiation well below the diffraction limit.
However, strong attenutation due to ohmic loss in metal allows for propagation at very short distances of the orders of 1-100 µm

## Slide 76
Plasmonic waveguides
Re(Ey)
Re(Hx)
Symmetric Asymmetric
Dielectrically supported Metal stripe SLOT (gap)
(=LOADED)
Metal–dielectric interface IMI (metal film) structure MIM structures
Low-index hybrid Wedge Channel (groove)

## Slide 77
Novel types of plasmonic waveguides
SOI “slot waveguide”
Hybrid dielectric-plasmonic slot waveguide (HDPSW)
PIROW – plasmonic inverted rib optical waveguide
C. Koos & al., Nat. Photonics 3(4), 16–219 (2009)
H. Benisty and M. Besbes, J. Appl. Phys. 108(6), 063108 (2010).
H.-S. Chu & al., J. Opt. Soc. Am. B 28(12), 2895 (2011) (others, too)
TE
R. F. Oulton & al., New J. Phys. 10, 105018 (2008)
??
R. F. Oulton & al., Nat. Photonics 2, 496 (2008);

## Slide 78
Hybrid dielectric-plasmonic slot waveguide
Basic geometric parameters
A: d = 100 nm
B: d = 200 nm
C: d = 300 nm
D: d = 400 nm
w = 150 nm
A: d = 100 nm
w = 150 nm
B: d = 200 nm
A: d = 100 nm
w = 150 nm

## Slide 79
Multimode interference coupler
1x2 MMI – simple configuration
1x2 MMI – improved configuration
1
2
3
1
2
3

## Slide 80
Mach-Zehnder interferometer
“On” state
“Off” state
J. Čtyroký et al.,, JEOS-RP vol. 8, 13021-13026 (2013).

## Slide 81
Waveguide structures with loss and gain
Asymmetric complex grating-assisted coupler
Basic theory:
L. Poladian, Phys. Rev. E, 54, 2963-2975, (1996).
M. Greenberg, M. Orenstein, Opt. Express, 12, 4013-4018, 2004.
M. Greenberg, M. Orenstein, Opt. Lett., 29, pp. 451-453, 2004.
M. Greenberg, M. Orenstein, IEEE JQE, 41, 1013-1023, 2005.
Application proposals:
M. Greenberg and M. Orenstein, PTL, 17, 1450-1452, 2005.
M. Kulishov et al, Optics Express, 13, 3567-3578, 2005.
Photonic analogues of quantum-mechanical “PT-symmetric” systems
First works:
H.-P. Nolting, M. Sztefka, J. Čtyroký, Proc. of IPR, Boston, 76-79, 1996.
G. Guekos, Ed., Photonic Devices for telecommunications, Springer, 1998, pp. 76-78. (“COST 240 Book”)
From the recent avalanche of papers:
R. El-Ganainy et al., Optics Letters, vol. 32, pp. 2632-2634, 2007.
K. G. Makris et al., Phys. Rev. Lett. vol. 100, pp. 103904(1-4), 2008.
J. Čtyroký et al., Optics Express, vol. 18, pp. 21585-21593, 2010.
C. E. Rüter et al., Nature Physics, vol. 6, pp. 192-195, 2010.
H. Benisty et al., Optics Express, vol. 19, pp. 18004-18019, Sep 2011.
A. A. Sukhorukov et al., Optics Letters, vol. 37, pp. 2148-2150, 2012.
J. Čtyroký, Opt. Quantum Electron. vol.46, 465-475, 2014.
…and many others…

## Slide 82
Asymmetric complex grating-assisted coupler
Grating-assisted directional coupler using asymmetric complex grating
or alternatively
complex, periodic in z
Fourier expansion contains only positive exponentials (“SSB modulation”)

## Slide 83
Asymmetric complex grating
Complex permittivity perturbation in individual grating segments:
or
The second option seems technologically simpler since it requires only two different values of and

## Slide 84
Let us consider the following ideal case of the grating at synchronism,
Then, the coupled equations read
we get the solution
For
for
Some more coupled-mode theory…

## Slide 85
ACGC is a reciprocal device!
Forward propagation
Backward propagation

## Slide 86
Numerical modelling (in-house 2D Fourier Modal Method)
Forward propagation
Backward propagation

## Slide 87
Straightforward ACGC applications
Wideband ADD multiplexor
M. Greenberg and M. Orenstein, PTL 17, 1450-1452, 2005
Light trapping in a ring resonator
(a “dynamic memory cell”)
M. Kulishov et al., OE 13, 3567-3578, 2005
grating “switched on”:
grating “switched off”:

## Slide 88
Coupled waveguides with loss & gain: historical remarks
H.-P. Nolting, M. Sztefka, J. Čtyroký, Proc. of IPR, Boston, 76-79, 1996.
G. Guekos, Ed., Photonic Devices for telecommunications, Springer, 1998, pp. 76-78. (“COST 240 Book”)

## Slide 89
guided waves
surface
wave
guided
waves
surface
wave
(TM)
mode
fields
“Rigorous” 2D analysis (planar waveguides)

## Slide 90
Eigenmode equation for TE modes
of a planar waveguide
Schrödinger equation for a particle in a 1D potential well
wave function
Formal analogy between a photonic waveguide and quantum-mechanical potential well
mode field distribution
wave number
mass; Planck constant
relative permittivity profile
effective refractive index
potential
particle energy
Loss/gain structure:
“PT symmetry”: complex potential,

## Slide 91
Balanced loss/gain “switching”:
Below
exceptional
point
Above
exceptional
point
gain channel
loss channel
C. E. Rüter et al. "Observation of parity–time symmetry in optics," Nature Physics, vol. 6, pp. 192-195, 2010.
Coupled waveguides with loss/gain

## Slide 92
Coupled waveguides with loss/gain
Below
exceptional
point
Above
exceptional
point
gain channel
loss channel
Fixed loss/variable gain switching:

## Slide 93
Plasmonic loss/gain structure
Hybrid dielectric-plasmonic slot waveguide directional coupler with gain section
Strongly unbalanced structure!
gain section
Only gain (εg” ) in the gain section is changed:

## Slide 94
Linear arrays of coupled waveguides with loss and gain
8 coupled channel waveguides
6 coupled channel waveguides
4 coupled channel waveguides
(quasi-TE polarization)

## Slide 95
“Circular” arrays of coupled waveguides with loss and gain
8 waveguides
6 waveguides
4 waveguides
(TE-like)

## Slide 96
Is there really anything new
under the Sun?
Yes! (hopefully…)
45 years of
Integrated Optics: